## Slide 1: Impact of high-power stress on dynamic ON-resistance of high-voltage GaN HEMTs
Donghyun Jin and Jesús A. del Alamo
Microsystems Technology Laboratory
Acknowledgement: ARPA-E ADEPT, SRC, DRIFT MURI

## Slide 2: Outline
Motivation
Dynamic ON-resistance measurement
High-power stress experiment
Discussion
Conclusion

## Slide 3: Motivation
Dynamic ON-resistance (RON) a.k.a. “current collapse”
Tirado et al, TED 2007

## Slide 4: Motivation
Dynamic ON-resistance (RON) a.k.a. “current collapse”
Primary concern in GaN power-switching and RF power-amplifier devices
Tirado et al, TED 2007

## Slide 5: Motivation
Much less understanding
Impact of electrical stress on dynamic RON
Especially, high-power (HP) state in GaN device operation

## Slide 6: Motivation
Much less understanding
Impact of electrical stress on dynamic RON
Especially, high-power (HP) state in GaN device operation
< RF-amplifier >
< Power-switching >

## Slide 7: Motivation
Much less understanding
Impact of electrical stress on dynamic RON
Especially, high-power (HP) state in GaN device operation
Meneghesso et al, TED 2006

## Slide 8: Motivation
Much less understanding
Impact of electrical stress on dynamic RON
Especially, high-power (HP) state in GaN device operation
Goal
New methodology for dynamic RON measurement
Investigate the impact of high-power stress on dynamic RON
Meneghesso et al, TED 2006

## Slide 9: Outline
Motivation
Dynamic ON-resistance measurement
High-power stress experiment
Discussion
Conclusion

## Slide 10: Dynamic RON measurement
New methodology for RON transient measurement from 200 ns to any arbitrary length of time
Auriga AU4750 pulsed-IV for RON(200 ns ≤ t ≤ 3 ms) + Agilent B1500A SDA for RON(3ms < t )

## Slide 11: Dynamic RON measurement
New methodology for RON transient measurement from 200 ns to any arbitrary length of time
Auriga AU4750 pulsed-IV for RON(200 ns ≤ t ≤ 3 ms) + Agilent B1500A SDA for RON(3ms < t )
Dynamic RON measurement from pulsed-IV

## Slide 12: Dynamic RON measurement
New methodology for RON transient measurement from 200 ns to any arbitrary length of time
VDS
t
VDSQ
VGS
1 V
t
VGSQ
Synchronous switching of VGS and VDS
Auriga AU4750 pulsed-IV for RON(200 ns ≤ t ≤ 3 ms) + Agilent B1500A SDA for RON(3ms < t )
Dynamic RON measurement from pulsed-IV

## Slide 13: Dynamic RON measurement
RON(t) from ID(t)-VDS measurements
Q(VGSQ= -10 V, VDSQ= 50 V)
ID(200 ns ≤ t ≤ 3 ms) @ VGS= 1 V, VDS ≤ 1.2 V

## Slide 14: Dynamic RON measurement
RON(t) from ID(t)-VDS measurements
Q(VGSQ= -10 V, VDSQ= 50 V)
1/RON
ID(t= 1 ms) @ VGS= 1 V
Extract RON transients from 200 ns up to 3 ms in OFF-to-ON
ID(200 ns ≤ t ≤ 3 ms) @ VGS= 1 V, VDS ≤ 1.2 V
100 μs
10 μs
200 ns

## Slide 15: Dynamic RON measurement
Pulsed-IV
Q(-5 V, 40 V)
RON_DC= 3.5 Ω∙mm
* Virgin GaN-on-SiC HEMT sample
200 ns ≤ t ≤ 3 ms

## Slide 16: Dynamic RON measurement
Pulsed-IV
Semiconductor Device Analyzer
200 ns ≤ t ≤ 3 ms
3 ms ≤ t ≤ 2.8 hr
Q(-5 V, 40 V)
RON_DC= 3.5 Ω∙mm
* Virgin GaN-on-SiC HEMT sample
OFF(-5 V, 40 V) to ON

## Slide 17: Dynamic RON measurement
Pulsed-IV
Semiconductor Device Analyzer
200 ns ≤ t ≤ 3 ms
3 ms ≤ t ≤ 2.8 hr
Q(-5 V, 40 V)
RON_DC= 3.5 Ω∙mm
RON transients over 11 decades in time → details in DJin ISPSD 2012
* Virgin GaN-on-SiC HEMT sample
OFF(-5 V, 40 V) to ON

## Slide 18: Outline
Motivation
Dynamic ON-resistance measurement
High-power stress experiment
Discussion
Conclusion

## Slide 19: High-power DC-stress
* Constant HP-stress: VDS= 20 V, ID≈0.6 A/mm, P≈12 W/mm tstress= 10, 20, 30, 40 min (4 samples)
Prominent degradation in RON and IDMAX; minor in IGOFF
Dynamic RON measurement after each HP-stress test
* tstress= 40 min sample

## Slide 20: Dynamic RON transients
Dynamic RON↑ ≥ 10 x RON_DC after 40 min HP-stress - Up to 30 min: minor increases in dynamic RON
In contrast, small RON_DC↑ (16%) - minor permanent (non-transient) degradation
Fast RON recovery in ms range in all cases
tstress= 40 min
30
20
10
Virgin
Transient from OFF (VGSQ= -10 V, VDSQ= 50 V) to ON (VGS= 1 V, VDS ≤ 1.2 V)
HP-stress time | RON_DC increase
10 | 7%
20 | 8%
30 | 11%
40 | 16%

## Slide 21: Time constant spectrum
40 min HP-stress → fast transient with short time constants (μs ≤ τ ≤ ms) ↑
In contrast, negligible changes in long time constants

## Slide 22: Dynamic RON at different T
As T ↑, RON transients substantially accelerated
RON transients → conventional traps
* tstress= 40 min sample

## Slide 23: Time constant spectrum at different T
Evolution of dominant time constant peaks at different T
* tstress= 40 min sample

## Slide 24: Arrhenius plot
Dominant trap energy levels at 0.31, 0.45, 0.53 and 0.57 eV (below EC of AlGaN barrier)
Responsible for dramatic increase in dynamic RON

## Slide 25: Outline
Motivation
Dynamic ON-resistance measurement
High-power stress experiment
Discussion
Conclusion

## Slide 26: Discussion: HP-stress with higher VDS
Virgin
After 3 min HP-stress with VDS= 30 V, P≈ 9 W/mm
Transient from OFF (-10 V, 50 V) to ON
Fast dynamic RON ↑ only in 3 min with lower P-level
Again, very fast RON recovery down to ms range
HP-stress with VDS↑ promotes fast dynamic RON degradation
After 20 min HP-stress with VDS= 20 V, P≈ 12 W/mm

## Slide 27: Discussion: Different epi-supplier
RON_DC= 3.5 Ω∙mm
* Red solid line: same GaN-on-SiC HEMT design processed in the same lot on nominally identical epitaxial wafer from different epi-supplier (denoted by epi-supplier II)
RON_DC= 4.6 Ω∙mm
Very different patterns of dynamic RON transient
virgin epi-supplier I
virgin epi-supplier II
Transient from OFF (-5 V, 40 V) to ON

## Slide 28: Discussion: HP-stress on epi-supplier II
IDMAX
RON
IGOFF
No prominent permanent degradation in RON, IDMAX and IGOFF - Large increase of IGOFF recoverable
* HP-stress on epi-supplier II device: VDS= 20 V, ID≈ 0.6 A/mm, P≈ 12 W/mm

## Slide 29: Discussion: Dynamic RON on epi-supplier II
2 hr HP-stress on epi-supplier II
Virgin epi-supplier II
Minor increase in dynamic RON up to 2 hr HP-stress
Epi-supplier II device more robust than epi-supplier I - RTH(thermal resistance) of epi-supplier II < RTH of epi-supplier I - Better heat dissipation through different buffer design
Epi-supplier II wafer more traps than epi-supplier I
OFF(-10 V, 50 V) to ON
40 min HP-stress on epi-supplier I

## Slide 30: Outline
Motivation
Dynamic ON-resistance measurement
High-power stress experiment
Discussion
Conclusion

## Slide 31: Conclusion
Developed new dynamic RON measurement methodology
Key findings from HP electrical stress - Large increase in dynamic RON on a short-time scale - Formation of shallow traps most likely inside the AlGaN barrier or at its surface
GaN HEMTs device operation under RF power or hard-switching conditions - Undesirable increase of dynamic RON on a very short time scale